Space product assurance

ECSS Secretariat

ESA-ESTEC

Requirements & Standards Division

Noordwijk, The Netherlands

End-of-life parameter drifts - EEE components

Foreword

This document is one of the series of ECSS Technical Memoranda. Its Technical Memorandum status indicates that it is a non-normative document providing useful information to the space systems developers’ community on a specific subject. It is made available to record and present non-normative data, which are not relevant for a Standard or a Handbook. Note that these data are non-normative even if expressed in the language normally used for requirements.

Therefore, a Technical Memorandum is not considered by ECSS as suitable for direct use in Invitation To Tender (ITT) or business agreements for space systems development.

Disclaimer

ECSS does not provide any warranty whatsoever, whether expressed, implied, or statutory, including, but not limited to, any warranty of merchantability or fitness for a particular purpose or any warranty that the contents of the item are error-free. In no respect shall ECSS incur any liability for any damages, including, but not limited to, direct, indirect, special, or consequential damages arising out of, resulting from, or in any way connected to the use of this Document, whether or not based upon warranty, business agreement, tort, or otherwise; whether or not injury was sustained by persons or property or otherwise; and whether or not loss was sustained from, or arose out of, the results of, the item, or any services that may be provided by ECSS.

Published by: 	ESA Requirements and Standards Division

ESTEC, P.O. Box 299,

2200 AG Noordwijk

The Netherlands

Copyright: 	2010© by the European Space Agency for the members of ECSS

Change log

| ECSS-Q-TM-30-12A 12 October 2010 | First issue |
| --- | --- |

Table of contents

Change log	3

Introduction	6

1 Scope and limitations	7

2 Normative references	8

3 Terms, definitions and abbreviated terms	9

3.1	Terms from other standards	9

3.2	Terms specific to the present document	9

3.3	Abbreviated terms	10

4 User responsibility	11

5 End-of-life parameter drift	12

5.1	General	12

5.2	Methodology	13

5.3	Applicability	13

5.4	Elements contributing to parameter drift	14

5.5	Other Elements contributing to parameter drift	14

6 End-of-life drift figures	15

6.1	General	15

6.2	Capacitors: ceramic – family-group code: 01-01 and 01-02	17

6.3	Capacitors: solid tantalum – family-group code: 01-03	18

6.4	Capacitors: non-solid tantalum – family-group code: 01-04	19

6.5	Capacitors: film – family-group code: 01-05	20

6.6	Capacitors: glass and porcelain – family-group code: 01-06	21

6.7	Capacitors: mica – family-group code: 01-07	22

6.8	Capacitors: feedthrough – family-group code: 01-10	23

6.9	Capacitors: semiconductor technology (MOS type) –  family-group code: 01-11	24

6.10	Capacitors: miscellaneous (variable capacitors) – family-group code: 01-99	25

6.11	Connectors – family-group code: 02-01, 02-02, 02-03, 02-07 and 02-09	26

6.12	Connectors RF – family-group code: 02-05	27

6.13	Piezo-electric devices: crystal resonator – family-group code: 03-01	28

6.14	Diodes – family-group code: 04-01, 04-02, 04-03, 04-04, 04-06, 04-08, 04-10 to 04-13, and 04-14	29

6.15	Diodes: RF/microwave – family-group code: 04-05, 04-11 to 04-13, 04-15, 04-16 and 04-17	32

6.16	Feedthrough filters – family-group code: 05-01	33

6.17	Fuses: Cermet (metal film on ceramic) – family-group code: 06-01	34

6.18	Inductors and transformers – family-group code: 07-01 - 07-03	35

6.19	Integrated circuits: logic – family-group code: 08-10, 08-20, 08-21, 08-29 to 08-42, and 08-80	36

6.20	Integrated circuits: non-volatile memories – family-group code: 08-22, 08-23 and 08-24	37

6.21	Integrated circuits: linear – family-group code: 08-50 to 08-60 and 08-69	38

6.22	Integrated circuits: linear converters – family-group code: 08-61 and 08-62	41

6.23	Integrated circuits: MMICs – family-group code: 08-95	42

6.24	Integrated circuits: miscellaneous – family-group code: 08-99	43

6.25	Relays and switches – family-group code: 09-01, 09-02 and 16-01	44

6.26	Resistors – family-group code: 10-01 to 10-11	45

6.27	Thermistors – family-group code: 11-01 to 11-03	49

6.28	Transistors: bipolar – family-group code: 12-01 to 12-04 and 12-09	50

6.29	Transistors: FET – family-group code: 12-05 and 12-06	52

6.30	Transistors: RF: bipolar – family-group code: 12-10, 12-11, 12-13	53

6.31	Transistors: RF: FET – family-group code: 12-12, 12-14, 12-15(FET), 12-16(FET)	54

6.32	Wires and cables – family-group code: 13-01 to 13 03	56

6.33	Opto-electronics – family-group code: 18-01 to 18-05	57

6.34	RF passive components: family-group-code: 30-01, 30-07, 30-09, 30-10 and 30-99	58

6.35	Fibre optic components: fibre and cable: family-group-code: 27-01	59

6.36	Hybrids	60

Annex A (informative) Family and group codes	61

Bibliography and reference documents	65

Introduction

This Technical Memorandum gathers end–of–life drifts in EEE component parameters suitable for worst case circuit analyses, when the current information is sufficient.

This Technical Memorandum gathers all data agreed by the Working Group during preparation of this document.

# Scope and limitations

This Technical Memorandum is suitable for all parties involved at all levels in the realization of space segment hardware and its interfaces.

The objective of this Technical Memorandum is to provide data about end-of-life parameter drifts and their use for equipment performance assessment up to the equipment end-of-life. To this end, the following are supplied:

- Estimation of end-of-life drifts due to ageing;

- Methodology guidelines and recommendations.

The reported ageing drifts in Clause 6 should not be confused with the endurance test drift limits allowed in the relevant ESCC specifications (table 4 or 6). The drift values reported here are based on effective life test results and extrapolated for operating temperature maxima respecting derating rules.

The selected data is derived from limited test samples, representative of the knowledge presently available as analysed by the ECSS WG.

End of life is one of the contributor of the Worst Case Circuit Analysis, others being Temperature, tolerance and radiation.

# Normative references

Bibliography and Reference documents in annex at end of document.

# Terms, definitions and abbreviated terms

## Terms from other standards

For the purposes of this document, the terms and definitions from ECSS-S-ST-00-01 apply.

## Terms specific to the present document

- ambient temperature

temperature surrounding a component

- case temperature

temperature on a component package surface

- hot spot temperature

highest measured or predicted temperature within any component

- junction temperature

temperature reached by a semiconductor within its active area during operation

- operating conditions

parameter stress and environment (temperature, vibration, shock and radiation) in which components are expected to operate

- performance

operation of a component or an equipment with respect to specified criteria

## Abbreviated terms

For the purpose of this document, the abbreviated terms from ECSS-S-ST-00-01 and the following apply:

| Abbreviation | Meaning |
| --- | --- |
| AC | alternating current |
| A/D | analogue to digital |
| AWG | American wire gauge |
| C | capacitance |
| DC | direct current |
| EMC | electro-magnetic compatibility |
| EPPL | European preferred parts list |
| EOL | end-of-life |
| ESCC | European Space Component Coordination |
| ESR | equivalent series resistance |
| f | frequency |
| FET | field effect transistor |
| GaAs | gallium arsenide |
| GEO | geostationary orbit |
| HBT | hetero-junction bipolar transistor |
| ISO | International Organization for Standardization |
| LED | light emitting diode |
| LEO | low Earth orbit |
| MEO | medium Earth orbit |
| MOS | metal on silicon |
| MIL (spec) | specification of the US Department of Defense |
| NASA | National Aeronautics and Space Administration |
| P | power |
| RadHard | radiation hardened |
| Ri | insulation resistance |
| SEBO | single event burn-out |
| SEGR | single event gate rupture |
| Si | silicon |
| SOA | safe operating area |
| Tj | junction temperature |
| Top | operating temperature |
| VCE | collector-emitter voltage |

# User responsibility

The user of this Technical Memorandum should verify that the ordered assurance level of procured components is compatible with the intended application.

# End-of-life parameter drift

## General

A worst-case circuit performance analysis is performed to assess the performance of an equipment at the end of its planned life.

- The present Technical Memorandum provides the time and temperature drift laws and the parameter drifts data when available at time of document drafting.

The laws and drifts are only provided in this document when they are validated.

- Temperature law is validated when drift data is available at least at three T°.

- Time law is validated only when drift measurements are available at several time intervals (more than two).

The designers should apply one of the following data sources:

- the present Technical Memorandum,

- or the drift after life test as defined in the procurement specification,

- or the drift from a representative set of life test data.

The applicability of the proposed life test data should be justified.

Data published by the manufacturer in the data sheet or application notes should be applied by order of precedence, on a case by case basis.

ECSS-Q-HB-30-01 provides extrapolation rules in the hypothesis that the time law is linear and the T° acceleration follows the Arrhenius law:

- For extrapolation to design life time one should refer to ECSS-Q-HB-30-01.

- For interpolation to design temperature one should refer to ECSS-Q-HB-30-01.

When a deviation to the present Technical Memorandum is encountered and approved on the basis of the drift from a representative set of life test data, an ECSS Change Request form (available from the ECSS Website).

The following additional text should appear in the Change Request:

“It is proposed to take into account the present deviation for further issue of the ECSS-Q-TM-30-12”

## Methodology

Drifts should be derived from test.

Key Test conditions parameters are:

- Junction Test Temperature

- Test Duration

- Sample statistics

Test conditions and duration should cover mission conditions and duration according to time law and acceleration laws.

Apply Arrhenius to extrapolate to lower operating junction temperature.

Apply referenced Ea or, preferably derive Activation energy Ea from test at two temperatures.

Time extrapolation law from test to mission durations should be validated. It should be based on three intermediate measurements, unless the pessimistic linear extrapolation is used.

When provided in percentage, the drift value provided in this Technical Memorandum was derived from the initial measured value or from the minimum or maximum specified as applicable.

In the application, this value should be applied in a WCCA on either the minimum or maximum limit specification, according to the drifts table.

## Applicability

The parameter degradation figures provided in this Technical Memorandum are suitable for all components procured in accordance with approved space specifications (ESCC, NASA, MIL, National Space Agencies, customer or manufacturer).

This Technical Memorandum is also suitable for other components that have undergone rigorous selection testing in accordance with ECSS-Q-ST-60.

## Elements contributing to parameter drift

This Technical memorandum only deals with the ageing (end-of-life factors).

- Component ageing and drifts (end-of-life factors)

The ageing of a component is a continuous process of physico-chemical change. In most cases, the rate of change is an exponential function of temperature. The figures provided in this Technical Memorandum take into account the most common degradation mechanisms.

## Other Elements contributing to parameter drift

In general, parameter drift comprises the following, unless otherwise specified.

- Initial tolerance

Parameter tolerance defined in the procurement specification.

- Temperature effects

The junction or case temperature which affects the component’s initial performance and contributes to the ageing mechanism.

- Voltage or current effects

The parameter degradation resulting from the applied voltage or current should be considered.

- Radiation effects

Semiconductors are susceptible to degradation due to radiation. A great disparity of behaviour can appear under the influence of radiation which can be caused by:

- mission orbit and duration,

- radiation types (such as protons, electrons and heavy ions),

- component technology, manufacturer, diffusion lot.

Identical components from different manufacturers can have a different radiation sensitivity.

- Component mounting

The mounting on a printed circuit board or substrate of surface mount components induces a stress that can have an influence on the component performance. Components sensitive to mounting processes are identified, but the expected change is not quantified as this is considered to be part of the evaluation of the device.

- Mission duration

Most parameter drifts are a function of time. The end-of-life parameter drift figures are valid for missions of up to 18 years provided the components are derated in accordance with ECSS-Q-ST-30-11 Standard.

# End-of-life drift figures

## General

This Clause provides

  - The drift laws and activation energies

  - The end-of-life parameter drift figures

  - A data integrity assessment.

Abbreviations used in the tables are explained in Clause 3.

Annex A contains a complete listing of the family and group codes for parts that are referred to in this Technical Memorandum.

The following format was used to collect and provide the data source references and statistics in order to raise the integrity level of this TM document.

Table 6-1: Table format for collection of data source reference

| Clause |  |  |  |
| --- | --- | --- | --- |
| Family-Code |  |  |  |
| Data source | Note (1) |  |  |
| Reference |  |  |  |
| Duration |  |  |  |
| Test flow | Note (2) |  |  |
| Thermal parameter | Note (3) |  |  |
| Temperature |  |  |  |
| Electrical Load Parameter | Note (4) |  |  |
| Load figure | Note (5) |  |  |
| # Manufacturers |  |  |  |
| # Lots |  |  | p |
| # Parts/ Lot |  |  | N |
| Mission life coverage | Note (6) |  |  |
| Confidence level indicator | Note (7) |  | 1/Square root of pN |
| (1) Data Source | Select between User industry, Parts Manufacturer , ESCC or Other |  |  |
| (2) Test flow | Select between ESCC Table #, Life tests, burn-in, Other. |  |  |
| (3) Thermal parameter | Select between Tc for passives or Tj for actives or unknown |  |  |
| (4) Electrical Test Parameter | Select between Voltage for Capa or Power for Resistors, or Other as applicable |  |  |
| (5) Load figure | Select between Voltage xVr for Capa or %Pn for Resistors, or Other as applicable |  |  |
| (6) Mission Life coverage | Maximum Life Duration derived from test data for derated junction or case temperature |  |  |
| (7) Confidence level indicator | Qualitative ranking based on square root of total Nber of parts |  |  |
|  | Low | Class 1_0.4: 1 to 6 parts |  |
|  | Fair | Class 0.4_0.2: 7 to 25 parts |  |
|  | Good | Class 0.2_0.1: 26 to 100 parts |  |
|  | High | Class 0.1_0: more then 100 parts |  |
| The Bibliography and reference documents, at the end of this document, contains a complete list of reference documents and data sources. |  |  |  |

## Capacitors: ceramic – family-group code: 01-01 and 01-02

### Drift laws

- Time law: unknown, linear one was used.

- Temperature law: Arrhenius law with Activation Energy: Ea=0,34 eV

### End-of-life drifts Type I and Type II:

| Capacitance ∆C/C | 55 °C | 85 °C | 110 °C |
| --- | --- | --- | --- |
| Type I |  |  |  |
| 10 years | 0,10 % | 0,28 % |  0,57 % |
| 18 Years | 0,18 % | 0,50 % |  1,02 % |
| Type II |  |  |  |
| 10 years | 0,19 % | 0,53 % |  1,14 % |
| 18 Years | 0,34 % | 0,96 % |  2,05 % |
| Insulation ∆R/R | 55 °C | 85 °C | 110 °C |
| Type I and Type II |  |  |  |
| 10 years | -50 % |  |  |
| 18 Years |  |  |  |
| Derived from test data at 125 °C, 3000 h , 2xUr |  |  |  |

### Data source and statistics

| Integrity assessment | Mission life coverage | 18 Years at 110 °C |
| --- | --- | --- |
|  | Confidence level indicator | Type I : Good |
|  |  | Type II: Good |

## Capacitors: solid tantalum – family-group code: 01-03

### Drift laws

- Time law: unknown, linear one was used.

- Temperature law: Arrhenius law with Activation Energy: Ea=0,19 eV

### End-of-life drifts

| Capacitance ∆C/C | 55 °C | 85 °C | 110 °C |
| --- | --- | --- | --- |
| 10 years | 0,63 % | 1,11 % |  1.67 % |
| 18 Years | 1,14 % | 2 % |  3 % |
| Leakage Current | 55 °C | 85 °C | 110 °C |
| 10 years | Maximum specified limit. |  |  |
| 18 Years |  |  |  |
| Derived from test data at 125 °C, 2000 h, 0.66xUr |  |  |  |

### Data source and statistics

| Integrity assessment | Mission life coverage | 18 Years at 110 °C |
| --- | --- | --- |
|  | Confidence level indicator | High |

## Capacitors: non-solid tantalum – family-group code: 01-04

### Drift laws

- Time law: unknown, linear one was used.

- Temperature law: Arrhenius law with Activation Energy: Ea= 0,43 eV

### End-of-life drifts

| Capacitance ∆C/C | 55 °C | 85 °C | 110 °C |
| --- | --- | --- | --- |
| 10 years | 4 % | 15 % |  37 % |
| 18 Years | 4 % | 15 % |  39 % |
| Leakage Current | 55 °C | 85 °C | 110 °C |
| 10 years | Maximum specified limit. |  |  |
| 18 Years |  |  |  |
| Derived from test data at 125 °C, 2000 hrs, Ur |  |  |  |

### Data source and statistics

| Integrity assessment | Mission life coverage | 18 Years at 110 °C |
| --- | --- | --- |
|  | Confidence level indicator | Good |

## Capacitors: film – family-group code: 01-05

### Drift laws

- Time law: unknown, linear one was used.

- Temperature law: Arrhenius law with Activation Energy: Ea= 0,22 eV

### End-of-life drifts

#### For Polycarbonate

| Capacitance ∆C/C | 55 °C | 85 °C | 100 °C |
| --- | --- | --- | --- |
| 10 years | 0,7 % | 1,35 % | 1,8 % |
| 18 Years | 0,78 % | 1,50 % |  2 % |
| Insulation ∆R/R | 55 °C | 85 °C | 100 °C |
| 10 years | -50 % |  |  |
| 18 Years |  |  |  |
| For information: derived from RAC data at 100 °C. |  |  |  |

#### For Polyethylene ( PET PM90, PM94, …)

| Capacitance ∆C/C | 55 °C | 85 °C | 100 °C |
| --- | --- | --- | --- |
| 10 years | 1,9 % | 3,7 % | 5 % |
| 18 Years | 2 % | 3,8 % |  5 % |
| Insulation ∆R/R | 55 °C | 85 °C | 100 °C |
| 10 years | -50 % |  |  |
| 18 Years |  |  |  |
| Derived from test data at 100 °C, 1.25xUr, 2000hrs for 80% load ratio |  |  |  |

### Data source and statistics

| Integrity assessment | Mission life coverage | Polycarbonate: unknown |
| --- | --- | --- |
|  |  | Polyethylene: 18 Years at 100 °C |
|  | Confidence level indicator | Polycarbonate: unknown |
|  |  | Polyethylene: High |

## Capacitors: glass and porcelain – family-group code: 01-06

### Drift laws

- Time law: unknown, linear one was used.

- Temperature law: Arrhenius law with Activation Energy: Ea= 0,37 eV

### End-of-life drifts

| Capacitance ∆C/C | 55 °C | 85 °C | 110 °C |
| --- | --- | --- | --- |
| 10 years |  0,02 % |  0,06 % | 0,13 % |
| 18 Years |  0,04 % |  0,10 % | 0,24 % |
| Derived from test data at 125 °C, 2xUr, 1000hrs for 60% load ratio.. |  |  |  |

### Data source and statistics

| Integrity assessment | Mission life coverage | 18 Years at 110 °C |
| --- | --- | --- |
|  | Confidence level indicator | Fair |

## Capacitors: mica – family-group code: 01-07

### Drift laws

- Time law

- Temperature law: Arrhenius law with Activation Energy: Ea= 0,37 eV

### End-of-life drifts

| Capacitance ∆C/C | 55 °C | 85 °C | 110 °C |
| --- | --- | --- | --- |
| 10 years |  0,10 % |  0,15 % | 0,33 % |
| 18 Years |  0,18 % |  0,27 % | 0,6 % |
| For information: derived from RAC data |  |  |  |

### Data source and statistics

| Integrity assessment | Mission life coverage | Unknown |
| --- | --- | --- |
|  | Confidence level indicator | Unknown |

## Capacitors: feedthrough – family-group code: 01-10

See Clause 6.2 Ceramic capacitors.

## Capacitors: semiconductor technology (MOS type) – 
family-group code: 01-11

### Drift laws

No data available.

### End-of-life drifts

No data available.

### Data source and statistics

No data available.

## Capacitors: miscellaneous (variable capacitors) – family-group code: 01-99

### Drift laws

- Time law: not applicable

- Temperature law : no thermal activation

- Activation Energy: not applicable

### End-of-life drifts

Stays within specification limit.

### Data source and statistics

No data available.

## Connectors – family-group code: 02-01, 02-02, 02-03, 02-07 and 02-09

### Drift laws

No drift should be considered.

### End-of-life drifts

No drift should be considered.

### Data source and statistics

No data available.

## Connectors RF – family-group code: 02-05

### Drift laws

No drift should be considered.

### End-of-life drifts

No drift should be considered.

### Data source and statistics

No data available.

## Piezo-electric devices: crystal resonator – family-group code: 03-01

### Drift laws

No drift law considered.

### End-of-life drifts

| Parameters | Drifts | Special conditions |
| --- | --- | --- |
| Crystals |  |  |
| Δf/f | Ageing specified in the detail specification. | Unless otherwise specified, ageing includes the expected total drift (including life-time, vibration, shock, drive level). Ageing should be added to the frequency tolerance at T0 and to the frequency variation over the operating temperature range. |
| Hybrid oscillators |  |  |
| Parameters applicable for the Logic Family components inside the hybride. |  | The variation applicable to the logic family inside the hybrid should be added to ageing. |

### Data source and statistics

No data available.

## Diodes – family-group code: 04-01, 04-02, 04-03, 04-04, 04-06, 04-08, 04-10 to 04-13, and 04-14

### Drift laws

- Time law: unknown, linear one was used

- Temperature law: Arrhenius with Activation Energy: Ea= 1,1 eV

### End-of-life drifts

#### Signal

No data available.

#### Switching

No data available.

| Forward Voltage | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years |  |  |  |  |
| 18 Years |  |  |  |  |

| Reverse Current | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years |  |  |  |  |
| 18 Years |  |  |  |  |

#### Rectifier

| Forward Voltage | 55 °C | 85 °C | 110 °C |
| --- | --- | --- | --- |
| 5 years |  |  | +1.4 % |
| 10 years |  |  |  |
| 18 Years |  | +0.45% |  |
| Reverse Current | 55 °C | 85 °C | 110 °C |
| 5 years |  |  | + 13% |
| 10 years |  |  |  |
| 18 Years |  | + 4.4% |  |
| Derived from Test data 2000 hrs, Tj=150°C |  |  |  |

#### Schottky

No data available.

#### Zener, non compensated reference

No data available.

#### Zener, compensated reference

| Zener Voltage | 55 °C | 85 °C | 110 °C |
| --- | --- | --- | --- |
| 10 years | 0 % | - 0,2 % |  |
| 18 Years |  |  |  |
| Reverse Current | 55 °C | 85 °C | 110 °C |
| 10 years | +0,4 % | +30 % |  |
| 18 Years |  |  |  |
| Dynamic Impedance | 55 °C | 85 °C | 110 °C |
| 10 years | -0,1 % / +0 % | -2.9 % / + 1.2 % |  |
| 18 Years |  |  |  |
| Derived from test data: at Ta= 100 °C, 3000 h, with Ea= 1.1 eV |  |  |  |

### Data source and statistics

#### Signal

No data available.

#### Switching

No data available.

#### Rectifier

| N | Mission life coverage | 18 Years at 85 °C |
| --- | --- | --- |
|  | Confidence level indicator | Fair |

#### Schottky

No data available.

#### Zener , non compensated reference

No data available.

#### Zener , compensated reference

| Integrity assessment | Mission life coverage | 18 Years at 55 °C |
| --- | --- | --- |
|  | Confidence level indicator | Good |

## Diodes: RF/microwave – family-group code: 04-05, 04-11 to 04-13, 04-15, 04-16 and 04-17

### Drift laws

- Time law:

- Temperature law:

- Activation Energy:

### End-of-life drifts for RF diode

#### Step recovery, varactor

No data available.

#### Schottky barrier

No data available.

### Data source and statistics

#### Step Recovery, Varactor

No data available.

#### Schottky barrier

No data available.

## Feedthrough filters – family-group code: 05-01

### Drift laws

No data available.

### End-of-life drifts

| Parameters | Drifts |
| --- | --- |
| Attenuation | -2 dB in addition to the initial tolerance. |
| DRi/Ri | -50 % |
| Information note. Attenuation: to be checked, in the meantime, drift is as proposed by ECSS-Q60 11A Insulation resistance: should be similar to Ceramic capacitor |  |

### Data source and statistics

No data available.

## Fuses: Cermet (metal film on ceramic) – family-group code: 06-01

### Drift laws

No data available.

### End-of-life drifts

No drift should be considered.

### Data source and statistics

No data available.

## Inductors and transformers – family-group code: 07-01 - 07-03

### Drift laws

No data available.

### End-of-life drifts

No drift should be considered.

### Data source and statistics

No data available.

## Integrated circuits: logic – family-group code: 08-10, 08-20, 08-21, 08-29 to 08-42, and 08-80

### Drift laws

No data available.

### End-of-life drifts

No drift should be considered.

### Data source and statistics

No data available.

## Integrated circuits: non-volatile memories – family-group code: 08-22, 08-23 and 08-24

### Drift laws

No data available.

### End-of-life drifts

No drift should be considered.

### Data source and statistics

No data available.

## Integrated circuits: linear – family-group code: 08-50 to 08-60 and 08-69

### Drift laws

- Time law

- Temperature law Arrhenius

- Activation Energy: Ea= 0,8 eV

### End-of-Life drifts

#### Relevant parameters for linear ICs

| Family code | Part type | Parameter | Code | Units |
| --- | --- | --- | --- | --- |
| Op Amp |  | Input Offset Voltage | V(IO) | % of max limit |
|  |  | Input Bias Current | I(B) | % of max limit |
|  |  | Input Offset Current | I(OS) | % of max limit |
|  |  | Large signal Voltage Gain | A(VO) | % of min limit |
|  |  | Gain BandWidth product | GBW | % of min limit |
|  |  | Common Mode Rejection Ratio | CMRR | % of min limit |
|  |  | Power Supply Rejection Ratio | PSRR | % of min limit |
|  |  | Supply Current | ICC | % of max limit |
| Comparator |  | Input Offset Voltage | V(IO) | % of max limit |
|  |  | Input Bias Current | I(B) | % of max limit |
|  |  | Input Offset Current | I(OS) | % of max limit |
|  |  | Large signal Voltage Gain | A(VO) | % of min limit |
|  |  | Supply Current | ICC | % of max limit |
| Regulator |  | Output Voltage |  |  |
|  |  | Reference Voltage |  |  |
|  |  | Line Regulation |  |  |
|  |  | Load Regulation |  |  |
|  |  | Input Offset Voltage | V(IO) | % of max limit |
|  |  | Input Bias Current | I(B) | % of max limit |
|  |  | Input Offset Current | I(OS) | % of max limit |
|  |  | Large signal Voltage Gain | A(VO) | % of min limit |
|  |  | gain band Width product | GBW | % of min limit |
|  |  | Supply Current | ICC | % of max limit |
|  |  | Overvoltage Protection Threshold | OVPTH |  |
|  |  | Undervoltage protection Threshold | UVPTH |  |
|  |  | Overcurrent protection threshold | OIPTH |  |
| PWM |  | Output Voltage |  |  |
|  |  | Reference Voltage |  |  |
|  |  | Line Regulation |  |  |
|  |  | Load Regulation |  |  |
|  |  | Input Offset Voltage | V(IO) | % of max limit |
|  |  | Input Bias Current | I(B) | % of max limit |
|  |  | Input Offset Current | I(OS) | % of max limit |
|  |  | Large signal Voltage Gain | A(VO) | % of min limit |
|  |  | gain band Width product | GBW | % of min limit |
|  |  | Supply Current | ICC | % of max limit |
|  |  | Overvoltage Protection Threshold | OVPTH |  |
|  |  | Undervoltage protection Threshold | UVPTH |  |
|  |  | Overcurrent protection threshold | OIPTH |  |
|  |  | Duty Cycle Max |  |  |
|  |  | Duty Cycle Min |  |  |
|  |  | Undervoltage protection hysterisis |  |  |
|  |  | Under voltage protection High |  |  |
|  |  | Under voltage protection Low |  |  |
| Voltage Reference |  | Reference Voltage |  |  |
|  |  | Line Regulation |  |  |
|  |  | Load Regulation |  |  |
| D/A converters |  | Full Scale current | IFS | mA |
|  |  | Zero Scale current | IZS | micro A |
|  |  | Supply Current | ICC | % of max limit |
| A/D converters |  |  |  |  |
| Analog Switch |  |  |  |  |
| Analog Multiplexer |  |  |  |  |
| Note 1: only DC relevant parameters are provided |  |  |  |  |
| Note 2: AC parameters definitions may also be useful |  |  |  |  |

#### Operational Amplifiers

| Input bias Current ( % of maximum limit) | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years | Covered by test data available |  |  |  |
| 18 Years | Covered by test data available |  |  |  |

The drifts values derived from Test referenced in RD3 show large dispersions from type to type.

The typical Test conditions reported at Ta=125 °C, 1000h, do not allow to cover the full Temperature-Duration spectrum.

With the assumption of Ea= 0,8 eV only the 55 °C, 18 years area is covered.

### Data source and statistics

| Integrity assessment | Mission life coverage | 18 Years at 55 °C |
| --- | --- | --- |
|  | Confidence level indicator | Unknown |

## Integrated circuits: linear converters – family-group code: 08-61 and 08-62

### Drift laws

No data available.

### End-of-life drifts

No data available.

### Data source and statistics

No data available.

## Integrated circuits: MMICs – family-group code: 08-95

### Drift Laws

To be defined.

To be organized depending on the RF functionality of the circuits.

### End-of-life drifts

To be defined.

To be organized depending on the RF functionality of the circuits.

### Data source and statistics

To be defined.

To be organized depending on the RF functionality of the circuits.

## Integrated circuits: miscellaneous – family-group code: 08-99

### Drift laws

Refer to relevant Integrated Circuit sections.

### End-of-life drifts

Refer to relevant Integrated Circuit sections.

### Data source and statistics

Refer to relevant Integrated Circuit sections.

## Relays and switches – family-group code: 09-01, 09-02 and 16-01

### Drift laws

Time law: not applicable.

Acceleration factor: operations number threshold.

### End-of-life drifts

| Parameters | Drifts |
| --- | --- |
| Contact resistance | Maximum limit (if N < 1 000 operations). Maximum limit × 2 (if N > 1 000 operations). |
| For thermal switches only:  Operating temperature (Tf)  Reset temperature (Tr) | Initial tolerance + 1 ºC Initial tolerance + 1 ºC |

### Data source and statistics

Not applicable.

## Resistors – family-group code: 10-01 to 10-11

### Drift laws – Generic to Resistors

Drift figures are presented in table format at Tcase + 50 %Pn.

As a preferable alternative, drifts should be reported in tables as a function of Hot Spot Temperatures 55 °C, 85 °C and 125 °C. This is on stand-by at time of production of this Technical memorandum.

All data, except for clause 6.26.2.6 Chip High Precision, is compiled manufacturer data for which confidence level could not be assessed.

- Time law: Cubic root of time law apply to all Metal and Film Resistors.

- Temperature law: Arrhenius with activation Energy Ea specified type by type.

### End-of-life drifts

#### Metal film (RNC except RNC90)

Time law: cubic root of time

Temperature law: Arrhenius, Ea= 0,28 eV

| Drifts at Tcase + 50 %Pn | 55 °C | 85 °C | 125 °C |
| --- | --- | --- | --- |
| 10 years | 0,19 | 0,44 % | 1,1 % |
| 18 years | 0,23 | 0,52 % | 1,3 % |
| Derived from compiled manufacturer Test data 8000 h at 125 °C, 100 % Pn , Drift 0,5 % Data published by the manufacturer in the data sheet or application notes should be applied by order of precedence, on a case by case basis. |  |  |  |

#### Metal film (RLR)

Time law: cubic root of time

Temperature law: Arrhenius, Ea= 0,28 eV

| Drifts at Tcase + 50 %Pn | 55 °C | 85 °C | 125 °C |
| --- | --- | --- | --- |
| 10 years | 0,39 | 0,88 % | 2,2 % |
| 18 years | 0,47 | 1,04 % | 2,7 % |
| Drifts derived from Test 8000 h 125 °C, 100 % Pn, Drift 1 % |  |  |  |

#### Foil (RNC90)

Time law: linear

A linear law is proposed for RNC90 for 0,3W, 125 °C.

Drift = 0,006t + 76,6

Temperature law: Arrhenius,Ea=0,18 eV

| Drifts at Tcase + 50 %Pn | 55 °C | 85 °C | 125 °C |
| --- | --- | --- | --- |
| 10 years | 0,02 % | 0,06 % | 0,08 % |
| 18 years | 0,02 % | 0,04 % | 0,11 % |
| Or R/R= 50 E-6 whichever is higher. |  |  |  |
| Drifts derived from Test 1000 h, 115 °C, 100 % Pn, Drift 50 E-6 |  |  |  |

#### Wire-wound power resistors (Type RWR, RER)

| Parameters | Drifts |  |  |
| --- | --- | --- | --- |
|  | 5 years | 10 years | 18 years |
| DR/R - wire-wound power: types RWR, RER | 0,8 % | 1,2 % | 1,5 % |

#### Chip Thin Film Resistor (Type RM), network Resistor;

Time law: cubic root of time

Temperature law: Arrhenius, Ea= 0,28 eV

| Drifts at Tcase + 50 %Pn | 55 °C | 85 °C | 125 °C |
| --- | --- | --- | --- |
| 10 years | 0,19 | 0,44 % | 1,1 % |
| 18 years | 0,23 | 0,52 % | 1,3 % |
| Drifts derived from Test 8000 h 125 °C, 100 % Pn, Drift 0,5 % |  |  |  |

#### Chip, Thin Film, high precision resistors (type UMA and PHR)

Time law: cubic root of time

Temperature law: Arrhenius, Ea= 0,28 eV

| Drifts at Tcase + 50 %Pn | 55 °C | 85 °C |  |
| --- | --- | --- | --- |
| 10 years | 0,04 % | 0,09 % |  |
| 18 years | 0,05 % | 0,11 % |  |
| Note 1: this data is superseded by the data provided in the detailed specification Note 2: EoL data does not account for the soldering process drift. Note 3: or R/R = 100 E-6 for NiCr Thin Film Chip whichever is higher. Note 4: derived from Test 8000 h, 85 °C, P=70mW, Drift 0,1 % |  |  |  |

#### Networks

Apply same drift values as the discrete counterparts.

#### Heaters

| Parameters | Drifts |  |  |
| --- | --- | --- | --- |
|  | 5 years | 10 years | 18 years |
| Heaters DR/R | ±0,6 % | ±0,8 % | ±1 % |

### Data source and statistics

#### Metal film (RNC except RNC90)

No data available.

#### Metal film (RLR)

No data available.

#### Foil (RNC90)

No data available.

#### Wire-wound power resistors (Type RWR, RER)

No data available.

#### Chip Thin Film Resistor (Type RM), network Resistor;

No data available.

#### Chip, Thin Film, high precision resistors (type UMA and PHR)

| Integrity assessment | Mission life coverage | 18 Years at 85 °C |
| --- | --- | --- |
|  | Confidence level indicator | High |

#### Networks

No data available.

#### Heaters

No data available.

## Thermistors – family-group code: 11-01 to 11-03

### Drift laws

No data available.

### End-of-life drifts

| Parameters | Drifts |  |  |
| --- | --- | --- | --- |
|  | Technology | Temperature |  |
|  |  | 0-100 °C | Other Temperature |
| Resistance PTC thermistor | Platinium Wire wound | Initial tolerance | Add ±0,5 % to the initial tolerance |
|  | Platinium Thin Film | No data available | No data available |
|  | Ceramic | No data available | No data available |
| NTC thermistor | Manufacturer data: Beta therm |  |  |

### Data source and statistics

No data available.

## Transistors: bipolar – family-group code: 12-01 to 12-04 and 12-09

### Drift laws

- Time law: linear, quadratic law to be checked

- Temperature law : Arrhenius, with activation Energy Ea= 0,7 eV

### End-of-life drifts

| Vce : ( %) | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years | 0,05 % | 0,38 % | 1,66 % |  |
| 18 Years | 0,09 % | 0,68 % | +3 % |  |

| Vbe : ( %) | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years | 0,02 | 0,13 % | 0,56 % |  |
| 18 Years | 0,03 % | 0,23 % | +1 % |  |

| Icbo : ( % ) | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years | +0,4 % | +9,8 % | +100 % |  |
| 18 Years | +0,7 % | +18 % | +180 % |  |

| Icbx : ( ) | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years |  |  |  |  |
| 18 Years |  |  |  |  |

Icbx : ( )

To be studied

| Gain : | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years |  |  |  |  |
| 18 Years | -0,13 % | -1,5 % | -7 % |  |

| BVceo, BVces, BVceo : ( % of specified minimum value) | 55 °C | 85 °C | 110 °C |  |
| --- | --- | --- | --- | --- |
| 10 years | No drift values are proposed for Breakdown Voltages which are treated in terms of derating |  |  |  |
| 18 Years |  |  |  |  |
| Data derived from Life Test 3000 h at Tj stress 200 °C Equivalent to 19 years at Tj=110 °C |  |  |  |  |

### Data source and statistics

| Integrity assessment | Mission life coverage | 18 years at 110°C |
| --- | --- | --- |
|  | Confidence level indicator | Good |

## Transistors: FET – family-group code: 12-05 and 12-06

### Drift laws

No data available.

### End-of-life drifts

- VGS(th) :  TBD %

- Igss : Within maximum specified value

- Idss : Within maximum specified value

- On-state resistance : Within maximum specified value

### Data source and statistics

No data available.

## Transistors: RF: bipolar – family-group code: 12-10, 12-11, 12-13

### Drift Laws

No data available.

### End-of-life drifts

No data available.

### Data source and statistics

No data available.

## Transistors: RF: FET – family-group code: 12-12, 12-14, 12-15(FET), 12-16(FET)

### Drift laws

For GaAs

Time law: Square root

Temperature law : Arrhenius

Activation Energy: Ea= 1.1 eV for Low level on Gain and Consumption.

Activation Energy: Ea= 1 eV for Power>1W on Consumption

### End-of-life drifts

#### Si FETs

| Parameters | Drifts |
| --- | --- |
| Pinch off voltage (Vp) | ±10 % |
| Gate leakage current (IGS) | 5 × worst case operational value |
| Drain current for VGS = 0 (IDSS) | Normally “ON”: ±20 % Normally “OFF”: 5 × initial value |
| Drain current for VGS threshold (IDS @ Vth) | Normally “ON”: 5 × initial value Normally “OFF”: ±20 % |
| Transconductance (gm) | ±25 % |
| Gain |  |
| Output Power |  |
| Data kept from former ECSS-Q60-11A for information only. |  |

#### Low level GaAs FETs

Relevant parameters:

Gain (dB per transistor stage)

Consumption ( %)

#### Power GaAs FETs (Pout <1W)

Relevant parameters:

Output Power (dB per transistor stage)

Consumption ( %)

Preliminary data.

### Data source and statistics

#### Si FETs

No data available.

#### Low level GaAs FETs

| Integrity assessment | Mission life coverage | 18 years, 115°C |
| --- | --- | --- |
|  | Confidence level indicator | Fair |

#### Power GaAs FETs (Pout <1W)

| Integrity assessment | Mission life coverage | 18 years, 115°C |
| --- | --- | --- |
|  | Confidence level indicator | Fair |

## Wires and cables – family-group code: 13-01 to 13 03

### Drift laws

No generic data available.

### End-of-life drifts

No generic data available.

### Data source and statistics

Generic.

## Opto-electronics – family-group code: 18-01 to 18-05

### Drift laws

No data available.

### End-of-life drifts

Relevant parameters.

| Parameters | Drifts |
| --- | --- |
| Light emitting diodes Light output power |  |
| Opto-coupler Ageing coefficient for current transfer ratio |  |
| Photo-transistor Collector leakage current (Iceo) |  |

### Data source and statistics

No data available.

## RF passive components: family-group-code: 30-01, 30-07, 30-09, 30-10 and 30-99

### Drift laws

No data available.

### End-of-life drifts

To be defined.

### Data source and statistics

No data available.

## Fibre optic components: fibre and cable: family-group-code: 27-01

### Drift laws

No data available.

### End-of-life drifts

To be defined.

### Data source and statistics

No data available.

## Hybrids

### Drift laws

No data available.

### End-of-life drifts

To be defined.

### Data source and statistics

No data available.

- (informative)
Family and group codes

This annex contains an extract from the European preferred parts list (EPPL) and it lists all the parts referred to in this Technical Memorandum providing their family and group codes.

| Family code | Group code | Family | Group |
| --- | --- | --- | --- |
| 01 | 01 | Capacitors | Ceramic |
| 01 | 02 | Capacitors | Ceramic Chip |
| 01 | 03 | Capacitors | Tantalum solid |
| 01 | 04 | Capacitors | Tantalum non-solid |
| 01 | 05 | Capacitors | Plastic metallized |
| 01 | 06 | Capacitors | Glass |
| 01 | 07 | Capacitors | Mica |
| 01 | 09 | Capacitors | Aluminium solid |
| 01 | 10 | Capacitors | Feedthrough |
| 01 | 11 | Capacitors | Semiconductor |
| 02 | 01 | Connectors | Circular |
| 02 | 02 | Connectors | Rectangular |
| 02 | 03 | Connectors | Printed circuit board |
| 02 | 07 | Connectors | Microminiature |
| 02 | 09 | Connectors | Rack and panel |
| 03 | 01 | Piezo-electric devices | Crystal resonator |
| 04 | 01 | Diodes | Switching |
| 04 | 02 | Diodes | Rectifier |
| 04 | 03 | Diodes | Voltage regulator |
| 04 | 04 | Diodes | Voltage reference/zener |
| 04 | 05 | Diodes | RF/microwave Schottky - Si |
| 04 | 06 | Diodes | Pin |
| 04 | 08 | Diodes | Transient suppression |
| 04 | 10 | Diodes | High voltage rectifier |
| 04 | 11 | Diodes | Microwave varactor - GaAs |
| 04 | 12 | Diodes | Step recovery |
| 04 | 13 | Diodes | Microwave varactor - Si |
| 04 | 14 | Diodes | Current regulator |
| 04 | 15 | Diodes | Microwave Schottky - GaAs |
| 04 | 16 | Diodes | RF/microwave - PIN |
| 04 | 17 | Diodes | Microwave GUNN - GaAs |
| 05 | 01 | Filters | Feedthrough |
| 06 | 01 | Fuses | All |
| 07 | 01 | Inductors | RF coil |
| 07 | 02 | Inductors | Cores |
| 07 | 03 | Inductors | Chip |
| 08 | 10 | Microcircuits | Microprocessors/microcontrollers/ peripherals |
| 08 | 20 | Microcircuits | Memory SRAM |
| 08 | 21 | Microcircuits | Memory DRAM |
| 08 | 22 | Microcircuits | Memory PROM |
| 08 | 23 | Microcircuits | Memory EPROM |
| 08 | 24 | Microcircuits | Memory EEPROM |
| 08 | 29 | Microcircuits | Memory others |
| 08 | 30 | Microcircuits | Programmable logic |
| 08 | 40 | Microcircuits | ASIC technologies digital |
| 08 | 41 | Microcircuits | ASIC technologies linear |
| 08 | 42 | Microcircuits | ASIC technologies mixed analogue/digital |
| 08 | 50 | Microcircuits | Linear operational amplifier |
| 08 | 51 | Microcircuits | Linear sample and hold amplifier |
| 08 | 52 | Microcircuits | Linear voltage regulator |
| 08 | 53 | Microcircuits | Linear voltage comparator |
| 08 | 54 | Microcircuits | Linear switching regulator |
| 08 | 55 | Microcircuits | Linear line driver |
| 08 | 56 | Microcircuits | Linear line receiver |
| 08 | 57 | Microcircuits | Linear timer |
| 08 | 58 | Microcircuits | Linear multiplier |
| 08 | 59 | Microcircuits | Linear switches |
| 08 | 60 | Microcircuits | Linear multiplexer/demultiplexer |
| 08 | 61 | Microcircuits | Linear analog to digital converter |
| 08 | 62 | Microcircuits | Linear digital to analogue converter |
| 08 | 69 | Microcircuits | Linear other functions |
| 08 | 80 | Microcircuits | Logic families |
| 08 | 99 | Microcircuits | Miscellaneous |
| 09 | 01 | Relays | Non-latching |
| 09 | 02 | Relays | Latching |
| 10 | 01 | Resistors | Metal oxide |
| 10 | 02 | Resistors | Wire-wound precision - including surface mount |
| 10 | 03 | Resistors | Wire-wound chassis mounted |
| 10 | 04 | Resistors | Variable trimmers |
| 10 | 05 | Resistors | Composition |
| 10 | 07 | Resistors | Shunt |
| 10 | 08 | Resistors | Metal film |
| 10 | 09 | Resistors | Chip - all |
| 10 | 10 | Resistors | Network - all |
| 10 | 11 | Resistors | Heaters, flexible |
| 11 | 01 | Thermistors | Temperature compensating |
| 11 | 02 | Thermistors | Temperature measuring |
| 11 | 03 | Thermistors | Temperature sensor |
| 12 | 01 | Transistors | Low power, NPN - < 2 W |
| 12 | 02 | Transistors | Low power, PNP - < 2 W |
| 12 | 03 | Transistors | High power, NPN - > 2 W |
| 12 | 04 | Transistors | High power, PNP - > 2 W |
| 12 | 05 | Transistors | FET N channel |
| 12 | 06 | Transistors | FET P channel |
| 12 | 09 | Transistors | Switching |
| 12 | 10 | Transistors | RF/microwave NPN low power/low noise |
| 12 | 11 | Transistors | RF/microwave PNP low power/low noise |
| 12 | 12 | Transistors | RF/microwave FET N-channel/P-channel |
| 12 | 13 | Transistors | RF/microwave bipolar power |
| 12 | 14 | Transistors | RF/microwave FET power - Si |
| 12 | 15 | Transistors | Microwave power - GaAs |
| 12 | 16 | Transistors | Microwave low noise - GaAs |
| 13 | 01 | Wires and cables | Low frequency |
| 13 | 02 | Wires and cables | Coaxial |
| 13 | 03 | Wires and cables | Fibre optic |
| 16 | 01 | Switches | Standard DC/AC power toggle |

| Family code | Group code | Family | Group |
| --- | --- | --- | --- |
| 18 | 01 | Opto electronics | Optocoupler |
| 18 | 02 | Opto electronics | LED |
| 18 | 03 | Opto electronics | Phototransistor |
| 18 | 04 | Opto electronics | Photo diode/sensor |
| 18 | 05 | Opto electronics | Laser diode |
| 27 | 01 | Fibreoptic components | Fibre/cable |
| 30 | 01 | RF passive devices | Coaxial couplers |
| 30 | 07 | RF passive devices | Isolator/circulator |
| 30 | 09 | RF passive devices | Coaxial power dividers |
| 30 | 10 | RF passive devices | Coaxial attenuators/loads |
| 30 | 99 | RF passive devices | Miscellaneous |

Bibliography and reference documents

# EEE manufacturer

- RD7 	Vishay VSD-TN0005-0407

# Agency

- RD3	Reports as per ESTEC Contract 13474/99/NL/MV

- RD4	RAC « Reliable application of Capacitor », RAC parts selection, application and control series, 1996.

- RD5	JPL reliability analyses handbook , D-5703

- RD6	CNES RO- CNE-RS-9065, WCA-DB, Ed1 -Rev0, December 1995

# Industry

- RD2 : Thales Alenia Space Company standard instruction and data base for dependability analysis. Ref.: 100141982F-EN-issue 2 (13 May 2007). Also proposed as common Astrium/Alcatel data base in meeting MOM/ECSS-Q-60-11/WG/OO1 , 18-19 march 04

# ECSS

- ECSS-Q-ST-30	Space product assurance - Dependability

- ECSS-Q-HB-30-01 	Space product assurance - Worst Case Circuit Analysis

- ECSS Q-ST-30-11	Space product assurance - Derating - EEE Component

- ECSS-E-ST-10-12	Space engineering - Method for calculation of radiation dose and margin policy

- gil1 : Space Product Assurance : Derating and end-of-life parameter drifts - Electrical, electronic and electromechanical components Ref.: ECSS-Q-60-11A (7 September 2004)

# Data source collection

- EoL_Data statistics_CNES_Diodes and Bipolar.zip, 30 July 2009

- Data source and Statistics for ECSS TM-30-12_RF FET_tas.xls, 05 October 2009

- Data source and Statistics for ECSS TM-30-12_Capa_ast.xls